## Slide 1: Building Better Foundations for Roads Using Emerging Technologies Soheil Nazarian, PhD, PE, DGE Macintosh Murchison Endowed Chaired Professor The University of Texas at El Paso
1
Notes: Good afternoon, Ladies and Gentlemen. It is such an honor and pleasure to deliver the 4th Proctor lecture to you from Sydney Australia. I would like to thank the members of TC203 and the International society for selecting me for this honor. The focus of my talk will be on how to improve the longevity of the roads and other transportation facilities by incorporating the old and new technologies that are not commonly used.

## Slide 2: Role of Transportation System
    Safety Smoothness Durability
Layers important to smoothness and durability
Notes: A typical pavement section consists of one or more surface layers being hot mix asphalt or concrete, often over a base (that can be stabilized) an optional subbase) and subgrade and natural soils. The focus of this talk is the foundation layers. These layers that significantly contribute to the smoothness and durability of the pavement structure are often not considered as important.

## Slide 3: Source of Problem
Flexible Pavements
Rigid Pavements
Notes: A quick survey of the literature quickly leads out to the understanding that the foundation layers are the source of a number of distresses. The focus of this talk is on two parameters the stiffness and uniformity of earthwork.

## Slide 4
Traditional Density-Based Compaction
They did the best they could with what was available to them
~70 years ago to solve a major problem
Engineering community pragmatically agreed that these tests
improve quality, even though not perfect
Notes: Let me reintroduce you to two of our superstars: Proctor in the left and Troxler in the right. Proctor introduced us with the concept of standard way of measuring density and optimum moisture content of different materials using a standard energy. Troxler introduced us to the concept of measuring the density using his nuclear density gauge based on the assumption that the density achieved in the Proctor mold will well represent the density of a roller going back and forth on a layer of soil.

## Slide 5
  Strength is not achieved by density alone.
  Optimum moisture is for compaction.
Proctor(1945), Trans 110, ASCE
  “No use is made of actual peak dry weight.”
  “Measure of soil compaction used is penetration resistance.”
Proctor Penetrometer
Famous Quotes of Ralph Proctor
Courtesy of John Siekmeier

## Slide 6: In Support of Proctor Quotes
±2% Change in MC = 5% Change in DD but Huge Change in Modulus

## Slide 7: We have come a long way since then in Design!!
1970’s
1990’s
2000’s
2010’s
Modulus!! Modulus!!

## Slide 8: We have come a long way equipment wise!!
1950’s
1970’s
1980’s
1990’s
2000’s
2010’s
Modulus!! Modulus!! Modulus!!
8

## Slide 9: We have come a long way in Pavement Analysis!!
1950’s
1970’s
1980’s
1990’s
2000’s
2020’s
Deflection?
Cool!!
How to use deflection?
I am not getting any younger!!
How to implement effectively?
What index to use for network level?
How to diagnose structural health?
Modulus!! Modulus!! Modulus!!

## Slide 10
We do not check whether the modulus designer assumed is achieved
We do not check whether the material selected provides the modulus assumed by designer
We assume Lab Moisture-Density Curve represents Field Compaction process
Construction Quality
Structural Design
Material Selection
Long Lasting Pavement
Yet the State of Practice in Earthwork!!
Not a good position to be

## Slide 11: Eventual Goal
to ensure that pavement lasts for a pre-defined life uniformly
One way to reach it:
Settle on a design methodology
(e.g., Pavement ME)
Define Parameters that are directly important to performance
(e.g., modulus)
Focus on these parameters
Transition from QAQC
to
Performance Management

## Slide 12: Appropriate Performance Management
Practical
Balance
Laboratory Testing Effort
Field Testing Effort
Analytical Modeling
Effort
Importance
of Project
Practicality

## Slide 13: Major Steps for Appropriate Performance Management
Selecting Suitable Material
Selecting Appropriate Design Parameters
Selecting Target Field Values
Conducting Field Process Control
Establishing Acceptance Process

## Slide 14: Selecting Suitable Material
A stiff/strong material does not correspond to a durable material.
Parameters, such as hardness of aggregates, percent fines and plasticity should be controlled for durability.
Do not abandon specifications on this subject

## Slide 15: Selecting Appropriate Design Parameters
Conducting laboratory resilient modulus tests before structural design
Utilizing results from a catalog of most common soils that have been tested
Estimating modulus based on calibrated models that are functions of index parameters
Using presumptive design values based on experience
Best Option Worst Option
Set Target Values using design algorithm
Set target Values using design algorithm
Estimate target values using test strip
Use traditional density based approach

## Slide 16: Selecting Target Field Moduli: Which Equipment?
Chart: Average Measured Modulus, ksi
| PSPA | Geogauge | Zorn LWD | Dynatest LWD
Average & Standard Deviation, ksi | 22.335 | 6.2115 | 3.4808 | 2.6711
n =20
COVs = 29±5%
ASTM E2583 LWD
ASTM E2835 LWD

## Slide 17
Can easily be part of design
Selecting Target Field Moduli
Input
  Thickness of each layer
  Poisson’s ratio of each layer
  Modulus of each layer
Output
  Target Deflection
Subgrade
Base
Subbase
17

## Slide 18
Chart: Moisture Content, %
| Dry | Optimum | Wet | Saturated
Field Moisture Content-Subgrade | 10.8083 | 15.775 | 16.1833 | 18.7542
OMC-Subgrade | 13.8 | 13.8 | 13.8 | 13.8
Impact of Moisture Content at Compaction
Chart: Modulus, ksi
| Saturated | Wet | Optimum | Dry
Dynatest LWD | 1.1396 | 1.3363 | 2.037 | 13.5036

## Slide 19: Field Process Control
Changes in material and moisture content have significant impact on modulus
Process control will ensure a more uniform and higher quality final product.
Quantifying variability is important to achieve uniformity
Need a strategy to manage variability
Need to ensure a rigid process control not less
Intelligent compaction can be used for this purpose
19

## Slide 20: Field Process Control: Manage Variability
Use statistics to manage variability
20

## Slide 21
Chart: Moisture Content at Testing
| 0.7 OMC | 0.8 OMC | 0.9 OMC | OMC | 1.1 OMC | 1.2 OMC
Compacted at 1.2 OMC | 136.6868 | 95.7905 | 44.0082 | 31.4678 | 18.3996 | 13.5487
Compacted at OMC | 101.6683 | 75.8774 | 47.5296 | 26.161
Compacted at 0.8 OMC | 32.4621 | 32.6079
Constant Density Specimens prepared at MDD
Field Process Control: Moisture Content

## Slide 22: Field Process Control: Unsaturated Soil Principles
Sr = w Gs rd/( Gs rw – rd)
Gs = specific gravity
rd = dry mass density
rw = mass density of water
Degree of Saturation, % | 120
 | 115
 | 110
 | 105
 | 100
 | 95
 | 90
 | 85
 | 80
 | 75
 | 70
 | 65
 | 60
 | 55
 | 50
 | 45
 | 40
 | 35
 | 30
 | 25
 | 20
 | 15
 | 10
 | 5
 | 0
 |  | Moisture Content, % |  |  |  |  |  |  |  |  |  | 
 |  | 5% | 7% | 9% | 11% | 13% | 15% | 17% | 19% | 21% | 23% | 25%
Dry Density, pcf | 90 | 15% | 22% | 28% | 34% | 40% | 46% | 53% | 59% | 65% | 71% | 77%
 | 95 | 17% | 24% | 31% | 38% | 45% | 52% | 59% | 66% | 72% | 79% | 86%
 | 99 | 19% | 27% | 35% | 43% | 50% | 58% | 66% | 74% | 81% | 89% | 97%
 | 104 | 22% | 31% | 39% | 48% | 57% | 66% | 74% | 83% | 92% | 101% | 109%
 | 109 | 25% | 35% | 45% | 55% | 65% | 75% | 85% | 95% | 105% | 115% | 125%
 | 115 | 29% | 40% | 52% | 64% | 75% | 87% | 98% | 110% | 121% | 133% | 145%
 | 121 | 34% | 48% | 61% | 75% | 88% | 102% | 116% | 129% | 143% | 156% | 170%
 | 127 | 41% | 57% | 74% | 90% | 106% | 123% | 139% | 155% | 172% | 188% | 204%
 | 133 | 51% | 71% | 91% | 111% | 131% | 152% | 172% | 192% | 212% | 233% | 253%
 | 140 | 65% | 91% | 118% | 144% | 170% | 196% | 222% | 248% | 274% | 300% | 327%
 | 147 | 90% | 127% | 163% | 199% | 235% | 271% | 308% | 344% | 380% | 416% | 452%
 | 154 | 143% | 200% | 257% | 314% | 371% | 428% | 486% | 543% | 600% | 657% | 714%

## Slide 23: Intelligent Compaction for Uniformity
CMV
CCV
MDP
Evib
Kb
VCV

## Slide 24
Traditional
CMV
2 – 33
34 – 44
45 – 74
Mean – 44
STDEV – 12
COV - 27%
CMV
14 – 30
31 – 39
40 – 58
Mean – 39
STDEV – 10
COV - 26%
CMV
COV of CMV
35 - 82
25 – 34
8 – 24
COV, %
Sublot Concept
Field Process Control: Uniformity
Gridding
Kriging

## Slide 25: Step 5: Acceptance Process
Based on moisture-adjusted deflection
dadj = dmeas / (Klab-field Kmoist )
Klab-field adjusts for differences in lab and field moduli at same moisture content and density
Kmoist adjusts for differences in compaction and testing moisture contents.
Include in
target value
for convenience

## Slide 26: Impact of Delay in Testing
Kmoist = eη(wC-wT)
η = 0.18 for subgrades
η = 1.19 for unbound aggregates
Chart: MCCompaction-MCTesting, %

## Slide 27
Field to lab Relationship
over 30 specimens

## Slide 28: Lab vs. Field Moduli
Chart: Normalized Lab
Chart: EFFRC/EFFRCopt
GP (1.33 OMC) | 2.4542 | 1.8194 | 1.3489 | 1 | 0.74136 | 0.54962 | 0.40747
GP (OMC) | 4.1866 | 2.5976 | 1.6117 | 1 | 0.62046 | 0.38497 | 0.23886
GP (96% of MDD) | 2.6755 | 1.9272 | 1.3883 | 1 | 0.72033 | 0.51888 | 0.37376
CL (1.2 OMC) | 1.5459 | 1.3369 | 1.1563 | 1 | 0.86485 | 0.74797 | 0.64689
CL (OMC) | 1.1922 | 1.1244 | 1.0604 | 1 | 0.94308 | 0.88939 | 0.83877
CL (96% of MDD) | 1.1204 | 1.0788 | 1.0386 | 1 | 0.9628 | 0.92699 | 0.89251
ML (OMC) | 1.0036 | 1.0024 | 1.0012 | 1 | 0.99881 | 0.99762 | 0.99643
ML (1.2 OMC) | 1.2336 | 1.1502 | 1.0725 | 1 | 0.93242 | 0.8694 | 0.81064
ML (96% of MDD) | 1.3109 | 1.1978 | 1.0944 | 1 | 0.91371 | 0.83486 | 0.76282
SC (OMC) | 1.1726 | 1.112 | 1.0545 | 1 | 0.94832 | 0.8993 | 0.85282
SC (1.2 OMC) | 1.1865 | 1.1208 | 1.0587 | 1 | 0.94459 | 0.89226 | 0.84282

## Slide 29
Service Life
12" Base +
8" LTS
12" Lime Treated Subgrade
12" Base
LWD
LWD
Backcalculation
+
Service Life Reduction
Simulation
Tandem Axle
Rutting
7.5” HMA
500 ksi
12” Base
50 ksi
12” LTS 10 ksi
Subgrade
Comparison
Red < 75%
Red < 75% of Average Value

## Slide 30
Chart: Station
| 0 | 25 | 50 | 75 | 100 | 125 | 150 | 175 | 200 | 225 | 250
 | 39.9678 | 44.0683 | 35.4736 | 37.9932 | 32.2605 | 30.6425 | 25.0665 | 40.5758 | 39.9284 | 37.9965 | 46.0794
 | 8.88 | 8.88
 | 11.1 | 11.1
Service Life Reduction
Chart: Station
| 150 | 125 | 100 | 75 | 50 | 25 | 0
 | 1.2841 | 1.169 | 0.52845 | 0.47793 | 0.51184 | 0.52091 | 0.42549
Premature Failure

## Slide 31: What is New and Exciting!!
Incorporating Intelligent Compaction in Performance Management
E (modulus)
k (stiffness)
CMV
CCV
HMV

## Slide 32
Need for Sophisticated Forward Model!!
32
Simulation of Roller Measurements
(Forward Model)
Roller Parameters
Material Types for Layers
Layer Properties
Chart: Deflection
Static vs. Dynamic
Stationary vs. Vibratory
Linear vs.
Nonlinear
Practicalities!!
How to trust model (Calibrate)
How to speed up (Machine Learning)

## Slide 33
Calibration of Model
Embedded
Geophones
h2
h1
Moving Direction
Ground DAQ
Chart: Distance from Drum, m
| -2.1287075552611112 | -1.9125627119808011 | -1.6612663108054171 | -1.358078451067497 | -1.0293013677532521 | -0.68531892058367405 | -0.34431575068507098 | 0 | 0.35447444042494602 | 0.71999609798800102 | 1.0751980280014231 | 1.432755260264579 | 1.8016360325579579 | 2.1344316598044699
Field Data | 0.061829 | 0.073355 | 0.084061 | 0.12374 | 0.12732 | 0.1623 | 0.24176 | 0.30325 | 0.26172 | 0.1619 | 0.094729 | 0.08747 | 0.08549 | 0.08568
FE Model | -0.0072122 | -0.0052303 | 0.0011772 | 0.013739 | 0.035644 | 0.072777 | 0.13569 | 0.24317 | 0.27941 | 0.32084 | 0.36779 | 0.42127 | 0.48143 | 0.54908 | 0.62431 | 0.70654 | 0.79788 | 0.89958 | 0.99099 | 1.0295 | 0.99167 | 0.90101 | 0.80007 | 0.70947 | 0.62796 | 0.55346 | 0.48652 | 0.42708 | 0.37432 | 0.32806 | 0.28732 | 0.25176 | 0.14673 | 0.085562 | 0.048697 | 0.024498 | 0.0054538 | -0.013188 | -0.032917
Geophone
Depths
FE Model
Drum
Pavement
Chart: Measured Displacement, mm
| 1.35 | 0.74 | 0.74 | 0.38 | 1.05 | 0.56000000000000005 | 0.63 | 0.32 | 0.67 | 0.33 | 0.28000000000000003 | 0.16 | 0.8 | 0.31 | 0.27 | 0.13 | 0.31 | 0.2 | 0.46 | 0.19 | 0.2 | 0.12 | 0.22 | 0.09 | 0.75 | 0.46 | 0.7 | 0.37 | 0.59 | 0.31 | 0.61 | 0.26 | 0.247 | 0.22 | 0.18 | 0.27 | 0.17399999999999999 | 0.14000000000000001 | 0.34 | 0.24 | 0.14000000000000001 | 0.37 | 0.28000000000000003 | 0.11
 | 3.1494 | 1.6643 | 1.5857 | 0.83506 | 2.4895 | 1.3137 | 1.7454 | 0.91958 | 2.5137 | 1.3266 | 1.6924 | 0.89145 | 1.15 | 0.57 | 1.12 | 0.61 | 0.3 | 0.26 | 0.75 | 0.54 | 0.16 | 0.12 | 0.84 | 0.7 | 2.3842 | 1.3943 | 2.3944 | 1.2693 | 1.4141 | 0.90277 | 2.9827 | 1.6404 | 1.7265 | 1.3973 | 0.90772 | 1.3264 | 1.1055 | 0.7267 | 1.2232 | 0.97442 | 0.63008 | 1.8363 | 1.5181 | 0.99409
Cleburne, TX: Stationary Test, Embankment | 3.1494 | 1.6643 | 1.5857 | 0.83506 | 2.4895 | 1.3137 | 1.7454 | 0.91958 | 2.5137 | 1.3266 | 1.6924 | 0.89145
MnROAD, MN: Moving Test, Subgrade | 2.3842 | 1.3943 | 2.3944 | 1.2693 | 1.4141 | 0.90277 | 2.9827 | 1.6404
Line of Equality | 0 | 8
Calibration
33

## Slide 34: Machine Learning as Forward Modeler
Artificial Neural Networks (ANN)
Instantaneous Responses
Material
Properties
Roller
Features
Pavement
Structure
INPUT
Chart: FE Surface Displacement, mm
Line of Equality | 0 | 20
+/- 10% Error Line | 0 | 22
+/- 10% Error Line | 0 | 18

## Slide 35: Estimation of E or k
Subgrade
Base
h
k‘1, k’2, k’3
k’2, k’3
d
Inputs
Operating
Conditions
Fev
Ddrum
ldrum
⁝
etc.

## Slide 36
Chart: LWD Modulus (MPa)
| 117 | 193 | 138 | 134
 | 140.8547 | 228.5607 | 183.0731 | 169.57
Line of Equality | 0 | 500
+/- 20% Uncertainty Bound | 0 | 738
+/- 20% Uncertainty Bounds | 0 | 492
Importance of Local Calibration
36

## Slide 37: Estimating Modulus using Artificial Intelligence
Chart: LWD Modulus, MPa
| 32.1 | 51.3 | 49.1 | 46.5 | 43.8 | 55.7 | 38.700000000000003 | 51.3 | 39.1 | 26.2 | 43.2 | 38.9 | 49.1 | 36.6 | 26.4 | 47.7 | 51.1 | 44.4 | 57.4 | 50.3 | 41.9 | 24.6 | 27 | 30.1 | 46.6 | 40.700000000000003 | 41.1 | 43.5 | 44.6 | 48.4 | 40.1 | 39.700000000000003 | 26.7 | 25.2 | 29.8 | 27.9 | 29.4 | 30.4 | 31.4 | 36.299999999999997 | 31.1 | 41.5 | 56.9 | 34.9
Site 1 | 37.508 | 51.622 | 49.9915 | 48.1591 | 47.4651 | 55.4011 | 42.1868 | 52.4739 | 42.167 | 32.294 | 46.3182 | 42.4238 | 49.7709 | 40.222 | 33.2987 | 49.6131 | 51.4294 | 46.4815 | 57.8278 | 51.8217 | 45.4021 | 32.5141 | 32.9407 | 37.3011 | 50.1743 | 45.8283 | 44.9422 | 47.6741 | 50.5763 | 54.8179 | 48.7758 | 46.8848 | 35.5893 | 32.4901 | 36.2429 | 34.2586 | 37.0796 | 37.5323 | 38.4805 | 45.2264 | 40.2668 | 50.4152 | 65.3546 | 43.1322
Site 2 | 85.4921 | 167.5832 | 69.1689 | 55.1316 | 172.8136 | 128.8802 | 50.2432 | 38.0321 | 47.7047 | 93.9901 | 97.1857 | 179.9551 | 229.3396 | 159.1652 | 140.2098 | 116.2994 | 61.5903 | 68.071 | 62.3918 | 110.557 | 139.0037 | 124.1191 | 187.4684 | 237.5424 | 172.917 | 194.215 | 191.8881 | 180.1501 | 166.5443 | 157.8889 | 140.0399 | 168.7751 | 160.3728 | 103.1408 | 200.7539 | 109.6895 | 232.8884 | 170.8576 | 265.6769 | 155.9135 | 102.374 | 180.1676 | 163.0875 | 100.2099
Site 3 | 224.8936 | 391.1004 | 301.3004 | 295.1674 | 197.0636 | 161.3015 | 229.7847 | 254.1849 | 227.1697 | 234.8276 | 178.2239 | 218.4045 | 329.9638 | 191.0707 | 297.3158 | 147.2621 | 317.5974 | 192.9045 | 241.9882 | 242.2761 | 160.8197 | 190.9797 | 235.9553 | 740.6929 | 260.2226 | 306.9025 | 133.4582 | 246.5534 | 482.215 | 355.0301 | 240.4784 | 277.1578 | 301.4247 | 232.9889 | 156.1075 | 171.8386 | 183.4944 | 263.5523 | 152.7876 | 137.7006 | 155.423 | 164.0501 | 129.0733 | 175.5123
Site 4 | 34.7828 | 47.3028 | 45.91 | 44.2681 | 43.6158 | 50.6484 | 38.9819 | 48.0729 | 38.9775 | 30.223 | 42.5708 | 39.1947 | 45.7022 | 37.2653 | 31.09 | 45.4964 | 47.1355 | 42.7808 | 52.8135 | 47.4858 | 41.7447 | 30.4007 | 30.7936 | 34.6268 | 45.9632 | 42.1442 | 41.3338 | 43.7779 | 46.304 | 50.0759 | 44.8039 | 43.0919 | 33.1421 | 30.4042 | 33.6705 | 31.9609 | 34.3993 | 34.8123 | 35.6821 | 41.708 | 37.3205 | 46.2658 | 59.4568 | 39.8386
Line of Equality | 0 | 1000
+/- 25% Uncertainty Bounds | 0 | 1250
+/- 25% Uncertainty Bounds | 0 | 750
Chart: Modulus, MPa
| STA +000 | STA +020 | STA +040 | STA +080 | STA +100 | STA +120 | STA +140 | STA +160 | STA +180
LWD Modulus | 38.9 | 50.2 | 36.6 | 39.7333 | 46.0667 | 42.5667 | 54.35 | 43.6333 | 26.2
Extracted Modulus | 42.4189 | 50.6943 | 40.2223 | 44.1441 | 48.6796 | 46.9541 | 55.1293 | 46.9384 | 32.294
20
40
80
100
120
140
160
200
0
Station, ft
R² = 0.98
SEE = 14 MPa

## Slide 38: Retrieved Modulus vs. LWD Modulus
Chart: LWD Modulus, MPa
| 122.29736767702337 | 234.49636510210416 | 194.17308107247595 | 112.96434070950009 | 314.74562960921185 | 310.87344403006517 | 71.97530691298337 | 39.485714285714288 | 43.083503092042278 | 126.23657487182633 | 66.89031859125852 | 225.86429850530217 | 86.597416981996389 | 40.755101197669028 | 43.083503092042278
Site 5: Subgrade | 119.9154 | 224.2048 | 212.0386 | 111.5005 | 302.9666 | 322.9569 | 77.3288 | 39.3177 | 41.7253 | 134.0983 | 64.5568 | 223.4931 | 83.627 | 40.3652 | 42.9296
Line of Equality | 0 | 600
+/- 30% Uncertainty Bounds | 0 | 420
+/- 30% Uncertainty Bounds | 0 | 780

## Slide 39
Concluding Remarks
Let’s us pragmatically work toward
implementing modulus-based technology
to improve further construction quality
even though not perfect
They did the best they could with what was available to
them ~70 years ago to solve a major problem
Engineering community pragmatically agreed that those
tests improve quality, even though not perfect

## Slide 40
More info!!

## Slide 41
Thank you!!
A number of colleagues and students
  Cesar Tirado
  Sergio Rocha
  Mehran Mazari
  Aria Fathi
41